#### Elastomeric Technical Data: Apron Caulk

Description :  Elastomeric flashing grade, brush able caulk which is excellent sealant for preparing fasteners, flashing, seams, skylights and other penetrations.

Color						:  White

Viscosity					:  Min. 140 KU @ 25C / 77F

Density, lbs. /gal				:  11.5

pH						:  >8

Percent Solids by Weight			:  63%±  1%

Flash Point					:  Same as water.

Hardness, Shore A				:  60-80 (ASTM D-2240)

Tensile Strength at Max Stress			:  200 p.s.i. @ 25C / 77F

500 p.s.i. @ -17C / 0F (ASTM D-412)

% Elongation at Break				:  500% @ 25C / 77F

400% @ -17C / 0F (ASTM D-412)

Permeability					:  5 perms / inch. 20 mil. Thick coating (ASTM E-389)

Coverage					:  5 gallons will cover 125lineal feet, 6 incheswide.

Recommended Coverage			:  As needed.

Minimum Surface Application Temperature	:  7.2C / 45F.  Do not allow to freeze.

Drying Time					:  3 hours @ 25C / 77F, 50% relative humidity.

Packaging					:  25 Kg Plastic Buckets

CAUTION : Do not apply within two hours of sunset, rain, fog or freezing temperatures. Apron Caulk  must be completely dry before  exposing to water or foot traffic.  Keep Apron Caulk  containers covered when not in use.  Dispose of all containers in accordance with state and local environmental regulations.  Keep away from children, If ingested, DO NOT induce vomiting.  Call Physician immediately

induce vomiting.  Call Physician immediately.